## Slide 1
Christopher G. Poulton
Interactions between sound and light on the nanoscale
Thursday 26th November, 2015
School of Mathematical and Physical Sciences, University of Technology Sydney (UTS), Australia
TexPoint fonts used in EMF.
Read the TexPoint manual before you delete this box.: AAAAAAA

## Slide 2
Research team
Christian Wolff
School of Mathematical Sciences, University of Technology Sydney (UTS)
Michael Steel
Department of Physics and Astronomy,
Macquarie University
Mike Smith, David Marpaung, Alvaro Casas-Bedoya and Benjamin J. Eggleton
School of Physics, University of Sydney

## Slide 3
Photonic crystal coupler-type switch
(Microphotonics group, St Andrews, UK)
Photonic crystal waveguide in chalcogenide (CUDOS)
Photonic crystal cavity resonator (CUDOS)
Structured materials in nanophotonics
Silicon
air
Photonic crystal fibre (Max Planck Erlangen, Germany)

## Slide 4
light
A Bragg grating is a one-dimensional periodic modulation of refractive index
An optical fibre confines light to the region in which it is slowest:

## Slide 5
The structure of the grating changes the relationship between energy and momentum of the wave
!
k
Photon
(!, k)
! = k c
“normal” relationship:
energy
momentum
Periodic structure relationship:
It’s complicated
Optical fibre

## Slide 6
The governing equations for light are Maxwell’s equations:
Assume all fields vary as
Refractive index
We have to solve the Helmholtz equation:

## Slide 7
Eigenvalues form a discrete set with no upper bound
Eigenfunctions form a complete set
For a finite domain with (say) Ã=0 on the boundary, we obtain a Sturm-Liouville eigenvalue problem:
Ã0
Ã1
Ã2
n(x)
x

## Slide 8
Periodic structures
We now consider the case where n(x) is a periodic function, with periodicity d.
The Bloch-Floquet theorem:
The quantity k is known as the Bloch wavenumber:
d
2d
3d
-d
n(x)
d
n(x)
ei k d

## Slide 9
The eigenvalue problem
with boundary conditions
is also a Sturm-Liouville problem, so the solutions form a discrete set for each k.
k
!
d
n(x)
ei k d

## Slide 10
Within a photonic band gap, there are no real eigenvalues.
What happens if we drive this structure with an incident wave at a frequency within the band gap?
frequency
!d /2¼c=0.395
Light
k
!

## Slide 11
Light

## Slide 12
Q: Can we create a nanophotonic circuit where a grating is
turned on or off?
A: we can, via a process called Stimulated Brillouin Scattering

## Slide 13
SBS fundamentals
Stimulated Brillouin Scattering
is a coherent interaction between vibrations and electromagnetic waves
The fundamental physical effects of the interaction are:
(Electric field causes material compression)
Light
Mechanical Deformation
Electrostriction
Photoelasticity
Optical field
Atomic lattice
(Compressive strain causes
change in refractive index)

## Slide 14
SBS fundamentals
Pump 1 w1
Intensity compresses material
Pump 2 w2=w1
Compression creates index grating
Excites acoustic wave frequency W
Pump 2 w2 = w1 - W
Pump reflected, down-shifted to w2
waveguide
Stimulated Brillouin Scattering (SBS)
The light resonantly excites an acoustic wave in the material.
B.J. Eggleton et al., Advances in Optics and Photonics 5 (2013), p536-587.
SBS leads to a narrow Stokes peak in the counter-propagating direction.
w1
Brillouin shift
W ~ 2 p x 7-11 GHz
Linewidth
GB ~ 2 p x 15-50 MHz
W
GB
Stokes gain

## Slide 15
Historical Perspective of SBS
SBS in optical fibres74
SBS in silicon55
SBS in WGM resonators76
SBS in wedge resonators52
On-chip SBS51
Year of discovery
First theoretical predictions1,65
First Brillouin laser2
Invention of the laser
First demonstration of SBS69
SBS in liquids70-72
SBS in gases73
SBS in PCF75
1920
2000
2010
1970
1980
1960
All references from B.J. Eggleton et al., Advances in Optics and Photonics 5 (2013), p536-587

## Slide 16
Applications of on-chip SBS
Pant et al. Optics Letters 2011.
Poulton et al. Optics Express 2012.
Slow/fast light
On-chip SBS laser
Kabakova et al. Optics Letters 2013.
Pant et al. Optics Letters 2013
Tuneable dynamic gratings
Microwave photonic filters
Byrnes et al. Optics Express 2012.
Non-reciprocal effects
On-chip SBS

## Slide 17
Theory
Materials and structures
3. Loss
Optical forces are complicated!
What works for light doesn’t work for sound
Fundamental limitations arise from nonlinear losses
Three big challenges:

## Slide 18
Theory: Solving the acoustic problem
Recall: to solve a mass-on-spring problem, we need:
Newton’s 2nd law
Hooke’s law
force
configuration
material

## Slide 19
Key concepts in elasticity:
Stress
Strain
Describes pressures acting throughout the body
Describes the mechanical distortion of a body
(potential -> force)
(configuration)
Elastic stiffness
(material)

## Slide 20
Strain describes the mechanical distortion of a solid body
Because it encapsulates the deformation of a box, the strain is a dimensionless second-rank tensor
extension in x
compression in y
pure shear
(volume unchanged)
u
The Iinearised strain comes from the first derivatives of u:

## Slide 21
Stress describes the pressures acting at all points in a solid
Stress is a second rank tensor that describes the direction of the force, and also the direction of the plane on which it is acting.
Positive normal stress Txx > 0
Negative normal stress Tyy < 0
Positive shear stress Txy > 0
x
y
z

## Slide 22
Hooke’s law
Stress
Strain
Hooke’s law states that stress and strain are linearly related.
The constitutive relationship involves a fourth-rank tensor
(unlike in EM theory, where it is rank 2)

## Slide 23
The main stiffness properties of isotropic materials are:
Units of Pa
Young’s modulus E
How hard it is to stretch
The bulk modulus K
How hard it is to compress
The shear modulus ¹
How hard it is to shear
Lame’s first parameter ¸
The Poisson ratio º
(dimensionless)
No real meaning
extension in y
compression in x
Any two of these completely specify the stiffness tensor.

## Slide 24
Newton’s second law for continuous bodies
Consider a small volume element with displacement u from equilibrium:
Force per unit volume
density
Displacement of volume element
Together with Hooke’s law
and boundary conditions, we can solve for any elastic problem.
Continuity of displacement, normal components of stress

## Slide 25
Types of solutions:
Bending modes
Twisting modes
Pressure modes

## Slide 26
Acoustic waves in nanophotonic waveguides
Acoustic mode
x
y
z
Restate Newton’s 2nd law:
Stress tensor
Substitute Hooke’s law:
where the strain is
strain tensor
½: density
(¸, ¹): Lamé parameters
and assume that the field u is harmonic in z:
displacement
Eigenvalue problem for , u

## Slide 27
x
y
z
We obtain the eigenvalue problem for :
where
and
Together with the boundary conditions

## Slide 28
Types of waves
Flexural Mostly shear
Torsional Mostly Shear
Longitudinal
Mostly longitudinal
Wave speed

## Slide 29
Coupling between optical and acoustic modes
Expand in mode fields:
Substitute into the appropriate PDEs
Assume 1) Slow-varying of amplitudes a and b, 2) coupling is locally weak and
3) acoustic waves are much slower than optical waves
Optical fields
Accoustic fields
With coupling terms:

## Slide 30
Theory of SBS: original formulation
Optical fields
Acoustic field
However: optical forces in materials (and at boundaries) are complicated!
E1
E2
Barnett, S. M., & Loudon, R. Phil. Trans. Roy. Soc. Lond. A 368, 927-939 (2010).
Original theory:
The coupling terms involve optical forces:
Electric fields
waveguide
Resulting boundary force

## Slide 31
Theory of SBS: new formulation
Optical fields
Acoustic field
New theory:
The coupling terms involve conserved field quantities on the boundaries:
waveguide
Equating these two formulation we show that each scattering process has a corresponding optical force

## Slide 32
Computed (longitudinal) mode of a As2S3 rib waveguide. Shading indicates the change in the material density, which determines the magnitude of Brillouin gain via electrostriction.
As2S3
140 nm SiO2 coating
SiO2
4 ¹m
Results (acoustic modes):
Results (optical modes):

## Slide 33
Result: Calculated Brillouin gain spectrum for a coated rib waveguide:
Incident light
Reflected light

## Slide 34
Applications of on-chip SBS
Pant et al. Optics Letters 2011.
Poulton et al. Optics Express 2012.
Slow/fast light
On-chip SBS laser
Kabakova et al. Optics Letters 2013.
Pant et al. Optics Letters 2013
Tuneable dynamic gratings
Microwave photonic filters
Byrnes et al. Optics Express 2012.
Non-reciprocal effects
On-chip SBS

## Slide 35
Slow-light on a chip
We can use Brillouin scattering to introduce a gain resonance in the counter-propagating direction:
Pump
Counter- propagating light
Due to causality, this gain must be accompanied by a change in the refractive index
!s
!as
!P
n(w)
n(w)
-g(w)
g(w)
w

## Slide 36
!s
!as
!P
n(w)
n(w)
-g(w)
g(w)
w
Velocity of a pulse:
Where ng is the group index:
Large change in refractive index
Strongly modified pulse velocities

## Slide 37
Schematic of experiment:
Pump !P
Input probe !s
t
Pump on
Pump off
t
Laser 1
Laser 2

## Slide 38
Actual experiment:

## Slide 39
Results: slowing of optical pulses
Increasing power

## Slide 40
Increasing power

## Slide 41
!s
!as
!P
n(w)
n(w)
-g(w)
g(w)
w
Slow light
“Backward light”
Phase measurements of group index:
Fast light

## Slide 43
Outlook
Future directions and open questions:
Is SBS feasible in CMOS-compatible materials?
The effect of 2D and 3D structure
Can we create an opto-acoustic “supermaterial”?

## Slide 46
On-chip slow and fast light
Slow-light on a chip
Pump
Counter- propagating light
Due to causality, this gain must be accompanied by a change in the refractive index
!s
!as
!P
n(w)
n(w)
-g(w)
g(w)
w
Max Delay = 22 ns
Max Advancement = 7 ns
Increasing power
Demonstration of slow-light on a chip:
Pant et al. Optics letters 37.5 (2012): 969-971.

## Slide 47
Challenges in SBS
Theory
Materials and structures
3. Loss
Optical forces are complicated!
What works for light doesn’t work for sound
Fundamental limitations arise from nonlinear losses
The grand vision: on-chip SBS in CMOS-compatible materials
However there are three big challenges:

## Slide 48
Theory of SBS: new formulation
Optical fields
Acoustic field
However: optical forces in materials (and at boundaries) are complicated!
e1
e2
Barnett, S. M., & Loudon, R. Phil. Trans. Roy. Soc. Lond. A 368, 927-939 (2010).
Theory: Modelling of the interaction can be done via coupled mode equations
The coupling terms involve optical forces:
Electric fields
waveguide
Resulting boundary force

## Slide 49
Theory of SBS: new formulation
Solution: avoid forces altogether.
From perturbation theory of Maxwell’s equations:
For reversible interactions it can be shown that
i.e. each scattering process has a corresponding optical force
Light
Mechanical Deformation
Electrostriction
Photoelasticity
C. Wolff et al. Stimulated Brillouin scattering in integrated photonic waveguides, accepted in Phys. Rev A, June 2015
Radiation pressure
Motion of boundaries

## Slide 50
For pressure waves, the governing equation is
Confinement possible from Total Internal Reflection
if vcore < vcladding.
Acoustic field (relative density change)
Sound velocity
The inverse sound velocity plays the role of acoustic refractive index
The acoustic field must be confined to the core
Propagation constant q
Frequency W
TIR region
W = v1 q
W = v2 q
i.e. the core must be less stiff than the cladding or substrate
Acoustic confinement

## Slide 51
Material requirements for guided SBS
Material requirements for SBS in waveguides:
Non-negligible photoelastic coefficients in core
High refractive index in core
Both acoustic and optical modes must be confined
The core must have a higher refractive index than the substrate, but be less stiff
What won’t work:
Silicon on silica (acoustic field lost to substrate)
What can work: Chalcogenides on silica

## Slide 52
A new challenge: nonlinear loss
Two-photon absorption excites carriers (2PA)
Carriers induce optical loss (FCA)
2PA leads to minimal direct loss, scales as I 2
FCA puts fundamental limits on the absolute gain
Wolff et al., accepted JOSA B, July 2015
Valence band
Excited carriers
FCA leads to large losses due to narrow linewidth of SBS, scales as I 3
2w
gain parameter
FOM:
2PA coefficient
FCA coefficient
Linear loss
FOM for Silicon nanobeam@1550nm: ~ 1.4
Maximal Stokes amplification: ~ 6dB

## Slide 53
New material systems
Proposal: Germanium in Silicon Nitride
High Gain in the mid IR (4 um).
Wolff, C., et al. Optics Express 22, p30735 (2014).
NB: anisotropy leads to large differences in gain
Soref, R. Nature Photonics, 4(8), 495–497 (2010) .

## Slide 54
New directions: metamaterials
The idea: dipole resonances between embedded
spheres enhance the interactions
Natural log of electrostriction enhancement for silver spheres in a chalcogenide matrix
Factor of 3.7 enhancement in electrostrictive constant
M. Smith et al., Phys. Rev. B 91, 214102 (2015).
Metamaterials can be used to enhance or suppress electrostriction

## Slide 55
Conclusions
Conclusions
Strong potential to engineer new materials for high SBS gain.
Nonlinear losses put critical limits on the applicability of SBS (silicon is particularly affected).
FOM:
Optical forces can be avoided in the theory
Acoustic guidance is critical, and what works for light does not always work for sound
Funding Sources
ARC Discovery Project (DP130100382)
CUDOS ARC Centre of Excellence (CE110001018)
ARC Laureate Fellowship (Prof. B.J. Eggleton, FL120100029)

## Slide 57
Historical Perspective of SBS
SBS in optical fibres74
SBS in silicon55
SBS in WGM resonators76
SBS in wedge resonators52
On-chip SBS51
Year of discovery
First theoretical predictions1,65
First Brillouin laser2
Invention of the laser
First demonstration of SBS69
SBS in liquids70-72
SBS in gases73
SBS in PCF75
1920
2000
2010
1970
1980
1960
All references from B.J. Eggleton et al., Advances in Optics and Photonics 5 (2013), p536-587

## Slide 58
Selection rules
The coupling between acoustic and optical modes is governed by simple selection rules
group C6v
C. Wolff, M.J. Steel, and C.G. Poulton. Optics Express 22, 32489-32501 (2014).